Product Data Sheet

Article designation:       photoluminescent pigment

Article No.               DS-T (축광)

Product group         inorganic photoluminescent pigments for visible                          effects

Main use              afterglowing plastic sheets silk screen printing

ink, Paints, textile ,etc.

Typical chemical properties

composition                      aikaline earth silicate

Formula:                         MeO. xAL₂O₃.ySiO₂:Eu

(Me=Ca, Mg, Sr, Ba; x =0.5-2.0, y=0.5-1.5)

Insoluble in                       Water, alkalies, organic solvents

Decomposition by                acids

Typical physical properties

Appearance                       yellowish

Specific gravity                   3.4g/㎤

Average Particle Size

As determined by Micromeritics Sedigraph    d₅₀=26.59μm

Temperature resistance               250 ℃

Typical luminescent properties

Exxitation                 UV radiation, white light(any visible light)

Excitation wavelength       200~450nm

Peak value                    520nm

Glowing Color              yellow-green

Brightness of afterglow        >12  hours

According to DIN67510, Part 1

축광 DS-T 시간대별 휘도

Brightness testing report

| Time (minutes) | Brightness(mcd/㎡) |
| --- | --- |
| 0 | 8561.6 |
| 1 | 1218.5 |
| 5 | 324.6 |
| 10 | 168.62 |
| 20 | 83.174 |
| 30 | 54.432 |
| 40 | 39.451 |
| 50 | 30.296 |
| 60 | 24.581 |

--------------------------------------------------------

Product Data Sheet  DS-F

Article designation:       photoluminescent pigment

Article No.               DS-F (슈퍼 장축광)

Product group         inorganic photoluminescent pigments for visible                          effects

Main use              afterglowing plastic sheets silk screen printing

ink, Paints, textile ,etc.

Typical chemical properties

composition                      aikaline earth silicate

Formula:                         MeO. xAL₂O₃.ySiO₂:Eu

(Me=Ca, Mg, Sr, Ba; x =0.5-2.0, y=0.5-1.5)

Insoluble in                       Water, alkalies, organic solvents

Decomposition by                acids

Typical physical properties

Appearance                       yellowish

Specific gravity                   3.4g/㎤

Average Particle Size

As determined by Micromeritics Sedigraph    d₅₀=53.67μm

Temperature resistance               250 ℃

Typical luminescent properties

Exxitation              UV radiation, white light(any visible light)

Excitation wavelength       200~450nm

Peak value                    520nm

Glowing Color              yellow-green

Brightness of afterglow        >12  hours

According to DIN67510, Part 1

슈퍼 장축광 DS-F 시간대별 휘도

Brightness testing report

| Time (minutes) | Brightness(mcd/㎡) |
| --- | --- |
| 0 | 10032 |
| 1 | 1401.6 |
| 5 | 381.19 |
| 10 | 210.85 |
| 20 | 111.81 |
| 30 | 78.02 |
| 40 | 58.982 |
| 50 | 47.441 |
| 60 | 39.617 |